HDPE - extrusion grade

Datasheet

| HDPE regrinds & washed blow molding. | Material |
| --- | --- |
| Solid Regrind / flakes. | Aspect |
| Mix color: yellow, transparent, pink, blue, green and black. | Color |
| Israel | Origin |
| Jerrycans | income |
| Post consumer waste. | Source |
| 39151000/5 | HS code |
| Sewage and drain pipe, silicon core pipe, infrastructures pipe, flexible pipe for electricians. | Applications |

| Method | Value | Parameter |
| --- | --- | --- |
| Visual | Flakes homogeneous | Aspect |
| 190ºc / 2.16 Kg | 0.2 – 0.5 g/10min | MFI |
| Laboratory | 0.940 - 0.960 | Density |
|  | 12 mm | Flakes size |
|  | up to 2% | Surface moisture |
| Mesh size 100µm | Very clean | Filter test |
|  | Up to 2% | Impurity pp |